Acetylenic Porphyrins:

Synthesis of Porphyrin Substituted

Tetraethynylethenes and

Polytriacetylenes

Для заказа доставки диссертации  воспользуйтесь поиском на сайте http://mydisser.com/ru/search.html?srchwhat=.

To order the delivery of the thesis use search on this site

http://mydisser.com/en/search.html?srchwhat=.

ACKNOWLEDGEMENTS

I wish to warmly thank Prof. Dr. François Diederich for the particular opportunity to

work in his research group, the proposition of the interesting and fascinating subject, and all

his support.

Furthermore, I want to express my gratitude to Dr. Rik Tykwinski for his very helpful

support in theory and in practice and for proofreading the manuscipt. His patience and

encouragement, as well as his remarkable ability to impart scientific knowledge was of

immense help and allowed me to rapidly deepen my understanding in the subject.

Special thanks go to Adrien Zingg, Rainer Martin, Martin Schreiber, Tilo Habicher, Dr.

Kevin Fitzpatrick, Dr. Jean-François Niergarten, Dr. Jennifer Wytko, and all of those who,

in one way or another, have contributed to aid me during my diploma thesis.

The exceptionally pleasant environment and working atmosphere in the ‘Diederich

Group’ helped to make my diploma thesis an unforgettable experience for me.

Zurich, 12th of June 1996 Volker Berl

Table of Contents

- I -

TABLE OF CONTENTS

1. ABSTRACT ...............................................................................1

2. INTRODUCTION ......................................................................2

3. GENERAL ASPECTS.................................................................5

3.1. Porphyrins..................................................................................... 5

3.1.1. General.......................................................................................................5

3.1.2. Nomenclature ...........................................................................................5

3.1.3. Some Selected Properties ........................................................................6

3.1.4. Natural Occurrence..................................................................................8

3.1.5. Synthetic Porphyrins ...............................................................................9

3.2. Tetraethynylethenes .................................................................... 11

3.2.1. Carbon Networks.....................................................................................11

3.2.2. Tetraethynylethene Nanoarchitecture and Generalities about

Conjugated Polymers ..............................................................................12

3.1.3. Tetraethynylethenes and Nonlinear Optics .........................................16

4. OBJECTIVES .............................................................................18

5. RESULTS AND DISCUSSION ....................................................24

5.1. Synthesis of the Iodinated Porphyrins...................................... 24

5.2. Synthesis of a Tetraethynylethene and a Hex-3-ene-1,5-

diyne Derivative........................................................................... 30

5.3. Synthesis of the Bis(porphinyl) Substituted TEE

Building Block............................................................................... 32

5.4. Synthesis of a Tetrakis(porphinyl) Substituted TEE............... 38

5.5. Synthesis of Porphinyl Substituted Polytriacetylene

Oligomers ...................................................................................... 39

5.6. Synthetic Approach towards an Interesting Fullerene-

Porphyrin Macrocycle ................................................................. 41

Table of Contents

- II -

5.7. Synthesis of a Linear Porphyrin-hex-3-en-1,5-diyne

Polymer.......................................................................................... 44

6. CONCLUSION AND OUTLOOK ...............................................46

7. EXPERIMENTAL SECTION .......................................................48

7.1. General Remarks .......................................................................... 48

7.2. Syntheses ....................................................................................... 50

8. REFERENCES AND NOTES.......................................................67

9. APPENDIX................................................................................71

9.1. Abbreviations................................................................................ 71

9.2. List of Products............................................................................. 73

Abstract

- 1 -

1. ABSTRACT

In this diploma thesis, the synthesis of laterally porphinyl substituted

polytriacetylene oligomers, linear porphinyl-hex-3-en-1,5-diyne oligomers, as well as

a tetrakis(porphinyl)tetraethynylethene is described. In addition, the synthesis of a

versatile building block, which could lead to the construction of a macrocyclic

fullerene-porphyrin structure, has been achieved.

Important steps towards the proposed target molecules were the synthesis of the

revised porphyrin system, its selective mono- and diiodination in meso-position with

[bis(trifuoroacetoxy)iodo]benzene and zincation of the latter to access the first two

important building blocks. In parallel, the synthesis of (E)-l,6-

bis[(triisopropylsilyl)ethynyl]hex-3-ene-l,5-diyne and (E)-3,4-bis[tert-butyldimethylsilyloxymethyl]

hex-3-ene-1,5-diyne from readily available starting materials has

been achieved. The modification and optimization of a procedure for acetylenic

palladium couplings using [Pd2(dba)3], AsPh3, and CuI led to the target molecules in

acceptable yields. Deprotection of the (E)-3,4-bis[(triisopropylsilyl)ethynyl)]-1,6-

bis[Zn(II)-5’,15’-bis(4’’-(ethyl-4’’’-butyryl)oxyphenyl)porphinyl]-hex-3-ene-l,5-diyne

and subsequent oxidative Glaser-Hay couplings successfully completed the route to

the desired oligomeric TEE derivatives. Although the quantities of the oligomers

necessary for complete characterization and study are still forthcoming, initial

investigations have established the ground work required for the realization of these

materials.

Introduction

- 2 -

2. INTRODUCTION

Tetrapyrrolic macrocycles such as porphyrins, chlorins, and bacteriochlorins are

vital to life on this planet. In fact, photosynthesis relies on the existence of the

chlorophyll and cytochrome porphyrins, by means of which photonic energy is

converted and stored as chemical energy. It is likely that cytochromes were

responsible for respiration long before oxygen was abundant in the Earth’s

atmosphere. With the advent of photosynthesis, the oxygen it produces is the

terminal electron acceptor for all aerobic respiration. It is this ability of

hemoproteins to then deal with the biochemistry of molecular oxygen that enables

cellular redox activity, not only by oxygen storage (monomeric myoglobin) and

transport (tetrameric hemoglobin) but also by electron transport (cytochromes) and

catalysis (oxygenases, peroxidases, etc).

This suggests the central role that porphyrins have played in chemical, biological

and physical research. Thus, massive contributions to our knowledge of the

structure and chemistry of porphyrins, metalloporphyrins, and related

compounds[1-3] were accumulated in the first half of this century. It was over 150

years ago that Verdeil converted chlorophyll to a red pigment prompting him to

suggest a structural relationship between chlorophyll, heme, and other porphyrins.

Shortly thereafter, Hoppe-Seyler strengthened this hypothesis by showing the spectral

resemblances between hematoporphyrin and an acid degradation product of

chlorophyll. The final steps in these structural elucidations were initiated by

Willstätter and culminated in the trailblazing work of Hans Fischer who

demonstrated the remarkable fact that but for the presence of two hydrogens, grass

would be coloured red and not green. Since then, the chemistry of porphyrins has

flourished into a vast and ever developing area of scientific endeavour. But natural

product chemists are no longer the only group interested in porphyrins. There is a

much larger constituency of chemists fascinated by the practical applications of

porphyrins to a wide diversity of fields.[3] In fact, the research carried out during

Introduction

- 3 -

this diploma thesis was not focused on the biological properties of porphyrins[4] but

on the synthesis of porphyrin systems with potential materials science and

technological applications.

To give the interested reader a brief, but by no means exhaustive insight into

current research being undertaken on sophisticated porphyrin systems, I would like

to mention the following topics: porphyrins designed to bind to electrodes and

surfaces,[5-7] porphyrin derived multi-electron reduction and oxidation catalysts,[8-18]

synthetic porphyrins as light harvesting antenna-systems,[19-21] porphyrinic materials

exhibiting nonlinear optical (NLO) properties,[19, 22-27] optical information storage

using porphyrins in matrices,[28-30] as well as possible porphyrin containing organic

electric conductors, semi- and superconductors,[28, 31] organic ferro-magnets,[32] and

liquid crystals.[33]

Compared to the relatively well investigated porphyrins, tetraethynylethene

(TEE) derivatives, the second important unit in my diploma thesis, are a class of

molecules only recently introduced. Though reported for the first time in 1969 by

Hori and co-workers[34] and synthetically advanced by Hauptmann in the mid-

1970’s,[35] tetraethynylethenes (TEEs) have only recently been developed.[36] Progress

in the early 1990’s by the works of Diederich et al.[37] then afforded TEEs with

virtually any desired substitution and protection patterns. TEEs are carbon rich,

rigid and very stable molecules, featuring undistorted full two-dimensional

conjugation and tolerating bulky pendant groups without loss of linear conjugation.

They are ideal precursors and building blocks for the design of new carbon

allotropes and networks, carbon-rich materials (e.g. polymers, molecular wires[38]),

as well as nanomaterials.[39, 40] Additionally, recent exciting studies on donoracceptor

substituted TEE compounds (so-called push-pull TEEs) have revealed their

interesting second and third order nonlinear optical properties and electrochemical

behaviour.[41]

In order to extend the present research[42, 43] towards the construction of

conjugated all-carbon backbone polymers by preparing polytriacetylenes (PTAs), it

was decided to link TEE compounds to porphyrins. The combination of the

chemistry and the chemical properties of these two types of compounds in one

Introduction

- 4 -

molecule was hoped to bring about new and interesting advanced materials for

electronic, photonic, and nonlinear optic applications.

In fact, the versatility of the TEE building block was fundamental to the planning

of the project carried out during my diploma thesis. The project was initiated by

Mark McLaughlin, an English undergraduate student, whose work targeted the

feasibility of synthesizing the proposed model systems. His success in achieving the

desired molecules encouraged the resumption of the investigations, pursuing them

to access the porphyrin substituted polytriacetylene oligomers.

8. REFERENCES AND NOTES

[1] K. D. Smith, Ed., Porphyrins and Metalloporphyrins, Elsevier, New York, 1975.

[2] D. Dolphin, Ed., The Porphyrins, Academic Press, New York, 1978, Vol. I - VII.

[3] R. H. Thomson, Ed., The Chemistry of Natural Products, 2nd Ed., Blackie A & P,

London, 1985.

[4] (a) P. J. Dandliker, F. Diederich, M. Gross, C. B. Knobler, A. Louati, E. M.

Sanford, Angew. Chem. 1994, 106, 1821-1824; (b) P. J. Dandliker, F. Diederich,

J.-P. Gisselbrecht, A. Louati, M. Gross, Angew. Chem. 1995, 107, 2906-2909;

[5] M. Yoneyama, A. Fujii, S. Maeda, T. Murayama, Chem. Lett. 1991, 929-932.

[6] F. Bedioui, S. G. Granados, J. Devynck, New J. Chem. 1991, 15, 939-941.

[7] D. K. Luttrull, J. Graham, J. A. DeRose, D. Gust, T. A. Moore, S. M. Lindsay,

Langmuir 1992, 8, 765-768.

[8] R. R. Durand, C. S. Bencosme, J. P. Collman, F. C. Anson, J. Am. Chem. Soc.

1983, 105, 2710-2718.

[9] J. P. Collman, J. E. Hutchinson, M. A. Lopez, R. Guilard, R. A. Reed, J. Am.

Chem. Soc. 1991, 113, 2794-2796.

[10] Y. L. Mest, M. L'Her, N. H. Hendricks, K. Kim, J. P. Collman, Inorg. Chem. 1992,

31, 835-847.

[11] C. K. Chang, I. Abdalmuhdi, Angew. Chem., Int. Ed. Eng. 1984, 23, 164-165;

Angew. Chem. 1984, 96, 154-155.

[12] P. S. Traylor, D. Dolphin, T. G. Traylor, J. Chem. Soc., Chem. Commun. 1984, 279-

280.

[13] T. G. Traylor, K. W. Hill, W. P. Fann, S. Tsuchiya, B. E. Dunlap, J. Am. Chem.

Soc. 1992, 114, 1308-1312.

[14] P. E. Ellis, J. E. Lyons, Coord. Chem. Rev. 1990, 105, 181-193.

[15] J. T. Groves, R. S. Myers, J. Am. Chem. Soc. 1983, 105, 5791-5791.

[16] D. Mansuy, P. Battioni, J. P. Renaud, R. Guerin, J. Chem. Soc., Chem. Commun.

1985, 155-156.

[17] Y. Naruta, F. Tani, N. Ishihara, K. Maruyama, J. Am. Chem. Soc. 1991, 113, 6865-

6872.

[18] K. Konishi, K. I. Oda, K. Nishida, T. Aida, S. Inoue, J. Am. Chem. Soc. 1992, 114,

1313-1317.

[19] J.-M. Lehn, Supramolecular Chemistry - Concepts And Perspectives, VCH,

Weinheim, 1995.

References

- 68 -

[20] M. Gouterman, P. M. Rentzepis, K. D. Straub, Porphyrins, ACS Symposium

Series 321, Washington, 1986.

[21] V. S.-Y. Lin, S. G. DiMagno, M. J. Therien, Science 1994, 264, 1105-1111.

[22] P. N. Prasad, D. J. Williams, Introduction to Nonlinear Optical Effects in Molecules

and Polymers, John Wiley & Sons, New York 1991, 243-245.

[23] G. H. Wagnière, Linear and Nonlinear Optical Properties of Molecules, VCH,

Weinheim, 1993.

[24] Ch. Bosshard, K. Sutter, Ph. Prêtre, J. Hulliger, M. Flörsheimer, P. Kaatz,

P. Günter, Advances in Nonlinear Optics - Organic Nonlinear Optical Materials,

Vol. 1, Gordon and Breach Publishers, Basel, 1995.

[25] H. S. Nalwa, Adv. Mater. 1993, 5, 341-358.

[26] D. V. G. L. N. Rao, F. J. Aranda, J. F. Roach, D. E. Remy, Appl. Phys. Lett. 1991,

58, 1241-1243.

[27] H. L. Anderson, S. J. Martin, D. D. C. Bradley, Angew. Chem. 1994, 106, 711-713,

Angew. Chem. Int. Ed. Engl. 1994, 33, 655-657.

[28] F. Vögtle, Supramoleculare Chemie, Teubner, Stuttgart, 1991.

[29] M. Pope, Mol. Cryst. Liq. Cryst. 1993, 228, 1-22.

[30] U. P. Wild, S. Bernet, B. Kohler, A. Renn, Pure Appl. Chem. 1992, 64, 1335-1342.

[31] J. Metz, M. Hanack, J. Am. Chem. Soc. 1983, 105, 828-830.

[32] J. S. Miller, J. C. Calabrese, R. S. McLean, A. J. Epstein, Adv. Mater. 1992, 4,

498-501.

[33] (a) B. A. Gregg, M. A. Fox, J. A. Bard, J. Chem Soc. Chem. Commun. 1987,

1134-1135; (b) B. A. Gregg, M. A. Fox, J. A. Bard, J. Am. Chem Soc. 1989, 111,

3024-3029.

[34] Y. Hori, N. Noda, S. Kobayashi, H. Tanigushi, Tetrahedron Lett. 1969, 3563-3566.

[35] (a) H. Hauptmann, Angew. Chem. 1975, 87, 490-491; (b) H. Hauptmann,

Tetrahedron Lett. 1975, 1931-1934; (c) H. Hauptmann, Tetrahedron 1976, 32, 1293-

1297.

[36] P. J. Stang, F. Diederich, Eds., Modern Acetylene Chemistry, VCH, Weinheim,

1995.

[37] Y. Rubin, C. B. Knobler, F. Diederich, Angew. Chem. Int. Ed. Eng. 1991, 30,

698-700; Angew. Chem. 1991, 103, 708-710.

[38] J.-M. Lehn, Angew. Chem. Int. Ed. Engl. 1988, 27, 89-112; Angew. Chem. 1988, 100,

91-116.

[39] F. Diederich, Nature (London) 1994, 369, 199-207.

[40] F. Diederich, Y. Rubin, Angew. Chem. 1992, 104, 1123-1146; Angew. Chem. 1992,

31, 1101-1124.

[41] (a) Ch. Bosshard, R. Spreiter, P. Günter, R. R. Tykwinski, M. Schreiber,

F. Diederich, Adv. Mater. 1996, 8, 231; (b) R. R. Tykwinski, M. Schreiber,

V. Gramlich, P. Seiler, F. Diederich, Adv. Mater. 1996, 8, 226-231.

References

- 69 -

[42] M. Schreiber, J. Anthony, F. Diederich, M. E. Spahr, R. Nesper, M. Hubrich,

R. Bommeli, L. Degiorgi, P. Wachter, P. Kaatz, Ch. Bosshard, P. Günter,

M. Colussi, U. W. Suter, C. Boudon, J.-P. Gisselbrecht, M. Gross, Adv. Mater.

1994, 6, 786-790.

[43] M. Schreiber, R. R. Tykwinski, R. Spreiter, Ch. Bosshard, P. Günther,

C. Boudon, J.-P. Gisselbrecht, M. Gross, U. Jonas, H. Ringsdorf, F. Diederich,

Adv. Mater. 1996, in preparation.

[44] W. Küster, Z. Physiol. Chem. 1912, 82, 463-483.

[45] H. Fischer, K. Seile, Ann. Chem. 1929, 468, 98-116.

[46] J. L. Soret, Compt. Rend. 1883, 97, 1267.

[47] A. Gamgee, Z. Biol. (Munich) 1897, 34, 505.

[48] A. Stern, G. Klebs, Ann. Chem. 1932, 500, 91-108; 1933, 504, 287-297; 1933, 505,

295-306.

[49] J. M. Osgerby and S. F. MacDonald, Can. J. Chem. 1962, 40, 1585-1589.

[50] P. S. Clezy, A. J. Liepa, A. W. Nichol, G. A. Smythe, Aust. J. Chem. 1970, 23,

589-602.

[51] A. D. Adler, F. R. Longo, J. D. Finarelli, J. Goldmacher, J. Assour, L. Korsakoff,

J. Org. Chem. 1967, 32, 476.

[52] G. M. Badger, R. L. N. Harris, R. A. Jones, J. M. Sasse, J. Chem. Soc. 1962,

4329-4337.

[53] G. H. Barnett, M. F. Hudson, K. M. Smith, Tetrahedron Lett. 1973, 2887-2892.

[54] H. Fischer, K. Platz, K. Morgenroth, Z. Physiol. Chem. 1929, 182, 265-288.

[55] P. Rothemund, J. Am. Chem. Soc. 1936, 58, 625-627.

[56] G. P. Arsenault, E. Bullock, S. F. MacDonald, J. Am. Chem. Soc. 1960, 82,

4384-4389.

[57] J. S. Lindsey, R. W. Wagner, J. Org. Chem. 1989, 54, 828-836.

[58] W. Krätschmer, L. D. Lamb, K. Fostiropoulos, D. R. Huffmann, Nature (London)

1990, 347, 354-362.

[59] A. M. Boldi, F. Diederich, Angew. Chem. Int. Edn. Engl. 1994, 33, 482;

Angew. Chem. 1994, 106, 482-485.

[60] W. R. Salaneck, I. Lundström, B. Rånby, Conjugated Polymers and Related

Materials, Oxford University Press, Oxford 1993.

[61] J. S. Miller, Adv. Mater. 1993, 5, 671-676.

[62] M. McLaughlin, Diplomarbeit 1995, ETH-Zürich.

[63] (a) M. Schreiber, Arbeitsbericht 1995; (b) S. G. DiMagno, V. S.-Y. Lin,

M. J. Therien, J. Am. Chem. Soc. 1993, 115, 2513-2515.

[64] B. Dietrich, P. Viout, J.-M. Lehn, Macrocyclic Chemistry - Aspects of Organic and

Inorganic Supramolecular Chemistry, VCH, Weinheim, 1993.

[65] W. A. Little, Sci. Am. 1965, 212 (2), 21-27.

[66] W. A. Little, J. Polym. Sci.: Part C 1967, 3-12.

[67] J. Bardeen, L. N. Cooper, J. R. Schreiffer, Phys.Rev. 1957, 108, 1175.

References

- 70 -

[68] J. M. Manriquez, G. T. Yee, R. S. McLean, A. J. Epstein, J. S. Miller, Science 1991,

252, 1415-1417.

[69] I. Z. Steinberg, E. Haas, E. Katchalski-Katzir in Time-Resolved Fluorescence

Spectroscopy in Biochemistry and Biology (R. B. Cundall, R. E. Dale, Eds.), Plenum

Press, New York 1983, 411-450.

[70] Th. Föster, Pure Appl. Chem. 1973, 34, 225-234.

[71] J. S. Manka, D. S. Lawrence, Tetrahedron Lett. 1989, 30, 7341-7344.

[72] R. Chong, P. S. Clezy, A. J. Liepa, A. W. Nichol, Aust. J. Chem. 1969, 22, 229-238.

[73] (a) R. W. Boyle, C. K. Johnson, D. Dolphin, J. Chem. Soc., Chem. Commun. 1995,

527-528. (b) Y. Ogato, K. Aoki, J. Am. Chem. Soc. 1968, 90,

6187-6191. (c) E. B. Merkushev, N. D. Simakhina, G. M. Koveshnikova,

Synthesis 1990, 486-487.

[74] E. Sanford, Dissertation, UCLA 1991.

[75] (a) J. Anthony, A. M. Boldi, Y. Rubin, M. Hobi, V. Gramlich, C. B. Knobler,

P. Seiler, F. Diederich, Helv. Chim. Acta 1995, 78, 13-45; (b) J. Anthony,

Dissertation, UCLA 1993.

[76] S. M. LeCours, H.-W- Guan, S. G. DiMagno, C. H. Wang, M. J. Therien, J. Am.

Chem. Soc. 1996, 118, 1497-1503.

[77] H. L. Anderson, C. J. Walter, A. Vidal-Ferran, R. A. Hay, P. A. Lowden, J. K. M.

Saunders, J. Chem. Soc., Perkin Trans. 1 1995, 2275-2279.

[78] R. W. Wagner, T. E. Johnson, F. Li, J. S. Lindsey, J. Org. Chem. 1995, 60,

5266-5273.

[79] C. Grant, P. Hambright, J. Am. Chem. Soc. 1969, 91, 4195-4198.

[80] X. Yan, D. Holten, J. Phys. Chem. 1988, 92, 5982-5986.

[81] 1H-NMR analysis supported this structure, although vigorous analysis was not

done.

[82] H. Imahori, Y. Sakata, Chem. Lett. 1996, 199-200.

[83] C. Bingel, Chem. Ber. 1993, 126, 1957-1959.